SPEC NOTE: This Guide Specification includes materials and installation procedures for a 2-ply SBS modified bitumen roofing membrane system over conventional insulated structural decks with air vapour barrier membrane in accordance with the requirements of the NBC for the building envelope.  Specifically, the base sheet layer is self-adhered to a prepared substrate followed by a torch applied cap sheet.  The self adhered base layer is intended to encapsulate all combustible substrates to provide a greater level of safety.  Adhesion of the base sheet is enhanced with the application of the torch applied cap sheet. This specification is ideally suited for premium performance roofing systems typical of Hospitals, Schools and commercial projects. This specification should be adapted to suit the requirements of individual projects. It is prepared in CSC three part format and should be included as a separate section under Division 7 - Thermal and Moisture Protection.

PART 1:  GENERAL

1.1		General Requirements

.1	The General Conditions, the Supplementary Conditions, the Instructions to Bidders and Division One General Requirements shall be read in conjunction with and govern this section.

.2	The Specification shall be read as a whole by all parties concerned.  Each Section may contain more or less than the complete work of any trade.  The Contractor is solely responsible to make clear to the Subcontractors the extent of their work.

1.2		Description

.1	Supply labour, materials, plant, tools and equipment to complete the Work as shown on the Drawings and as specified herein including, but not limited to the following:

.1	Concrete Roof Deck (by others),

.2	Primer & Air - Vapour Barrier Membrane,

.3	Roof Insulation & Tapered Insulation,

.4	Self-Adhered Base Sheet & Self-Adhered Base Sheet Flashing,

.5	Heavy Duty Cap Sheet & Cap Sheet Flashing,

.6	Metal Flashings and Accessories.

1.3		Related Work

.1	Concrete:			Section [XXXXX]

.2	Rough Carpentry:		Section [XXXXX]

.3	Metal Flashing and Trim:	Section [XXXXX]

.4	Sealants:			Section [XXXXX]

.5	Roof Vents & Drains:		Section [XXXXX]

1.4		References

.1	CSA A123.4-[M1979]:		Bitumen for use in Construction of Built-Up Roof Coverings and 	Dampproofing and Waterproofing systems.

.2	CAN/CSA-A247-[M86]:		Insulating Fibreboard.

.3	CSA 0121-[M1978]:		Douglas Fir Plywood.

.4	CAN/CGSB-37.9-[83]:		Primer, Asphalt, Unfilled for Asphalt Roofing, Dampproofing and 	Waterproofing.

.5	CAN/ULC-S704-01:		Standard Specification for Thermal Insulation, Polyurethane and 	Polyisocyanurate Boards, Faced.

.6	CAN/ULC-S770-00: 		Standard Test Method for Determination of Long Term Thermal 	Resistance (LTTR) of Closed Cell Thermal Insulating Foams

.7	CAN/CGSB-37.29-[M89]:		Rubber-Asphalt Sealing Compound.

.8	CGSB 37-GP-56M 9th Draft:	Membrane, Modified, Bituminous, Prefabricated, and Reinforced 	or Roofing.

1.5		Shop Drawings

.1	Submit shop drawings in accordance with Section [XXXXX] - [XXXXX].

.2	Provide complete layout for tapered insulation system.

1.6		Storage and Handling

.1	Store modifiedPLUS( membranes and accessories in a dry location, in original containers.

.2	If product is stored outside, it must be elevated on a platform and be protected with a waterproof cover, which will shed water away from the material.

.3	Store all products in an upright position. Do not double stack unless product is on pallets and packaged as received from factory. Place a minimum of 12mm thick OSB panel between stacked pallets. Never stack more than two pallets high without racking.

.4	In cold weather store modifiedPLUS( membranes in heated area and take onto roof immediately prior to use.

.5	Store adhesives and primers between 15°C (60°F) and 26°C (80°F), or restore to temperature range before use.

.6	Store combustible materials away from heat and open flame.

.7	Do not store modifiedPLUS( membranes at ambient temperatures above 49°C (120°F).

1.7		Environmental Requirements

.1	modifiedPLUS( installations in temperatures below 4°C (40°F) can result in quality concerns.

.2	Verify adhesion regularly during cold temperature applications.

.3	Store rolls in heated location until needed on the roof.

.4	It is recommended that when temperatures remain below –10°C (4°F) for mopping or self-adhesive applications and below –18°C (0°F) for thermofusible applications operations should be suspended.

.5	Minimum working temperatures shall take into consideration a factor for wind chill. Application temperature shall be considered to be the temperature minus half of the wind speed as recommended by the Canadian Roofing Contractors Association (CRCA).

1.8		Protection

.1	Maintain a fire watch for a minimum of two hours following completion of each day’s termination of thermofused application.  Check for hot spots using infrared temperature gauge.

.2	Maintain one fully operational fire extinguisher per torch applicator within 10 m of point of work.

.3	Protect membrane from site damage during and post application. Cover traffic areas with appropriate protection to serve as walkways to prevent any damage to the membrane.

1.9		Submittals

.1	Submit in writing, a document stating that the applicator of the primary membranes specified in this Section is recognized by the manufacturer as suitable for the execution of the Work.

.2	Prior to commencing the Work submit copies of manufacturers’ current ISO 9001- 2008 certification. Membrane, primers, sealants, adhesives and associated auxiliary materials shall be included.

.3	Prior to commencing the Work submit references clearly indicating that the membrane manufacturer has successfully completed projects on an annual basis of similar scope and nature for a minimum of fifteen years.  Submit references for a minimum of ten projects.

.4	Prior to commencing the Work submit manufacturers’ complete set of standard details for the air/vapour barrier and roofing membrane systems showing a continuous plane of air tightness throughout the building envelope.

1.10	Quality Assurance

.1	Perform Work in accordance with the printed requirements of the membrane manufacturer and this specification. Advise designer of any discrepancies prior to commencement of the Work.

.2 	Maintain one copy of manufacturers literature on site throughout the execution of the Work.

.3	At the beginning of the Work and at all times during the execution of the Work, allow access to site by the roofing membrane manufacturers representative.

.4	At the request of the [architect] [engineer] [consultant], submit documentation certifying that the roofing membranes comply with CGSB 37-GP-56M.

.5	Materials used in this Section, including air/vapour barrier membranes, roofing membranes, primers, mastics, adhesives and sealants shall be fully compatible and shall be sourced from one manufacturer.

.6	At the request of the [architect] [engineer] [consultant], submit copies of the membrane manufacturers current certification to ISO 9001-2008.

1.11  	Alternates

.1 	Submit requests for alternates in accordance with Section [XXXXX] - [XXXXX].

.2	Alternate submission format to include:

.1	Submit evidence that alternate materials meet or exceed the performance characteristics of Product requirements and documentation from an approved independent testing laboratory certifying that performance of the roofing membrane system including the air barrier and transition sheet membrane, exceeds the requirements of the National Building Code.

.2	Submit copies of manufacturer's current ISO 9000 certification.

.3	Submit references clearly indicating that the membrane manufacturer has successfully completed projects on a annual basis of similar scope and nature for a minimum of five years.

.4		Submit manufacturers’ complete set of standard details for the roofing membrane systems showing a continuous plane of air tightness throughout the building envelope.

.3	Submit requests for alternates to this specification a minimum of fifteen (10) working days prior to tender closing for evaluation. Include a list of 10 projects executed over the past five years.

.4	Acceptable alternates will be confirmed by addendum. Substitute materials not approved in writing prior to tender closing shall not be permitted for use on this project.

1.12	Warranty

.1	For the Work of this Section, the 12 months warranty period prescribed in subsection GC 32.1 of General Conditions “C” is extended to [24 months] [60 months].

.2	Contractor hereby warrants the modified bituminous roofing and membrane flashings for leak coverage in [accordance with GC24], but for two years.

.3	Roofing membrane manufacturer hereby warrants the membrane and membrane flashings for leak coverage as a result of faulty materials for a period of [five years] [ten years]. Scope of warranty shall include material required to return the membrane to a watertight condition.

.4	Roofing membrane manufacturer hereby warrants that the membrane and membrane flashings for leak coverage as a result of faulty materials or faulty workmanship for a period of ten [10] years. Scope of warranty shall include material and labour required to return the membrane to a watertight condition.

PART 2:  PRODUCTS

# 2.1	Components and membrane materials must be obtained as a single-source from the membrane manufacturer to ensure total system compatibility and integrity.

2.2	Roofing Membrane Manufacturer: 	Henry Company Canada,

15 Wallsend Drive

Scarborough, ON  M1E 3X6

Tel: 1-800-387-9598

Fax: 1-877-890-4866

Web Site: www.ca.henry.com

2.3		Adhesive Primers

.1	Adhesive primer for all self-adhered base sheet flashings shall be Tack Sheet Adhesive 930-38 manufactured by Henry - Bakor and be fully compatible with membranes.

.2	Adhesive Primer all self-adhered transition air/vapour barrier membranes shall be Blueskin( Adhesive manufactured by Bakor and be fully compatible with membranes.

2.4		Roof Deck Air/Vapour Barrier Membranes

.1	Air/vapour barrier membrane shall be Vapor-Bloc( SA, Self-Adhered Air/vapour Barrier manufactured by Henry - Bakor; an SBS modified bitumen self-adhering membrane with a blue polyethylene film, and having a minimum thickness of 0.8 mm (30 mils).

2.5		Roof Insulation Adhesive

.1	Cold adhesive for adhering polyisocyanurate insulation to Vapor-Bloc( SA shall be Thermostik( 880-33, Non-Flammable Roof Insulation Adhesive manufactured by Bakor, a fast setting, moisture and fungus resistant synthetic rubber adhesive, minimum application temperature        -10˚C.

.2    	Cold adhesive for adhering insulation to Vapor-Bloc( SA shall be Thermostik( 840-10, Internal Setting Roofing Adhesive manufactured by Bakor, a fast setting, 100% solids, solvent free, 2 component elastomeric rubber adhesive, minimum application temperature not to exceed –10 ˚C.

2.6		Roof Insulation

.1	Roof Insulation:  Closed-cell HCFC FREE “Green” polyisocyanurate foam core manufactured using ACUltra Hydrocarbon blowing agent and integrally laminated to thick, durable and dimensionally stable inorganic coated-glass facers with a nominal weight of 800 grams/m2. Compressive strength 20 psi conforming to ASTM C 1289, Type II, Class 1, CCMC No. 12464-L, CAN/CGSB-51.26-M86, CAN/ULC-S704.  ACFoam IV manufactured by Atlas Roofing Corporation and represented by Building Resource Inc, www.buildingresource.ca, phn: 416-410-4055.

.2	Roof Coverboard:  Closed-cell HCFC FREE “Green” polyisocyanurate foam core manufactured using ACUltra Hydrocarbon blowing agent and integrally laminated to thick, durable and dimensionally stable inorganic coated-glass facers with a nominal weight of 800 grams/m2.. Compressive strength minimum 90 psi conforming to CAN/ULC-S704, 0.5 inch thick (12.7mm), providing thermal Resistance (LTTR) of R2.5.  ACFoam HS CoverBoard manufactured by Atlas Roofing Corporation and represented by Building Resource Inc, www.buildingresource.ca, phn: 416-410-4055.

2.7		Tapered Roof Insulation as fabricated with a minimum thickness of 25 mm (1/2 inch) and minimum slope of 1:50 (2%).

2.8		Self-Adhered Base Sheets and Base Sheet Flashings

.1	Base sheet and base sheet flashing (Self-Adhered) shall be modifiedPLUS( NP180 Tack Sheet manufactured by Henry – Bakor a self-adhered SBS modified bitumen membrane having a minimum thickness of 3.0 mm (120 mils) and a non-woven polyester reinforcement Complies with CGSB 37-GP-56M, Type 2, Class C, Grade 2.  The upper surface shall have a polyethylene film and the lower surface shall be self-adhering with a siliconized release film.

.2	Base sheet and base sheet flashing (Self-Adhered) shall be modifiedPLUS( G100 Tack Sheet manufactured by Henry - Bakor, a self-adhered SBS modified bitumen membrane having a minimum thickness of 2.0 mm (80 mils) and a non-woven glass fibre reinforcement. Complies with CGSB 37-GP-56M, Type 2, Class C, Grade 1.  The upper surface shall have a polyethylene film and the lower surface shall be self-adhering with a siliconized release film.

2.9		Thermo-fused Cap Sheet and Cap Sheet Flashing

.1	Cap sheet and cap sheet flashing shall be modifiedPLUS HD gT4 manufactured by Henry-Bakor an SBS modified bitumen membrane having a nominal thickness of 4 mm (160 mils) and a composite reinforcement.  Complies with CAN CGSB 37-GP-56M, Type 2, Class A, Grade 2.

.2	The upper surface shall have ceramic granules and the lower surface shall have a polyethylene film.

.3	Physical Properties when tested in accordance with CGSB 37-GP-56M 9th draft:

Strain Energy			MD 14.2 kN/m (81 lbf/in)

XD 13.0 kN/m (74 lbf/in)

Tensile Strength		MD 19.0 kN/m (108 lbf/in)

XD 16.0 kN/m (91 lbf/in)

Ultimate Elongation		MD 152%

XD 160%

Tear Strength			64 N (14.4 lbf)

Water Resistance		Pass water tightness

Water Absorption		0.59 g

Water Vapour transmission	0.02 g/m²•24h

Dynamic Impact (Puncturing)	Pass

Static Puncturing		Pass

Lap Joint Strength:

-after 5 days @ 23˚C		806 N (181 lbf)

-after 5 days @ 50˚C (H2O)	908 N (204 lbf)

-after 5 days @ 50˚C (H2O) &

5 cycles of freeze thaw		921 N (207 lbf)

Dimensional Stability		MD 0%, XD 0%

Accelerated Weathering 		Pass

1080 2 h cycles

Crack Bridging				> 10 cycles at -20˚C (-4˚F)

Low Temperature Flexibility

at -30˚C (-22˚F)

Initial - 			No sign of cracking

90 days @ 70˚C 		No sign of cracking

2.15	Membrane sealant in compliance with CAN/CGSB 37.29, shall be POLYBITUME( 570-05 Polymer Modified Sealing Compound manufactured by Henry – Bakor

2.16	Exposed Sealant for Membrane and Metal Flashing

.1	Sealant shall be HE925 BES Sealant manufactured by Henry-Bakor, a moisture cure, medium modulus polymer modified sealing compound having the following physical properties:

.1			Compatible with sheet air barrier, roofing and waterproofing membranes and substrate,

.2	Complies with Fed. Spec. TT-S-00230C, Type II, Class A,

.3	Complies with ASTM C 920, Type S, Grade NS, Class 25,

.4	Elongation: 450 – 550%,

.5	Remains flexible with aging,

.6	Seals construction joints up to 25mm wide.

2.17	Plastic Roof Cement in accordance with of CAN/CGSB-37.5. shall be Bakor 810-21 Wet/Dry Plastic Roof Cement.

2.18	Pitch Pocket Filler shall be Thermostic( 840-10 Internal Setting Roof Adhesive, a non-shrink 100% solids pourable filler in conjunction with Blueskin( Spray Prep manufactured by Henry - Bakor.

PART 3:  EXECUTION

3.1		Examination: Verify that all deck surfaces and substrates are acceptable for installation of the system.

3.2		Self-Adhered Air/Vapour Barriers

.1	Apply primer by roller or spray to all surfaces to be covered with self-adhered vapour block as required and allow to dry.

.2	Unroll and align transition membrane centered at low point of roof or drain.  Apply membrane by removing release paper providing 50 mm (2 inches) side and end laps.

.3	Apply membrane complete and continuous to prepared and primed substrate in an overlapping shingle fashion and in accordance with manufacturer's written instructions.  Stagger all end laps by a minimum of 450 mm (18”).

.4	Promptly roll all laps and membrane with a weighted roller to effect the seal.

3.3		Insulation application over Vapor Bloc SA

.1	Embed insulation in cold adhesive beads 20 mm wide spaced at 300mm (3/4’ beads @12”). Increase coverage at perimeters to 20mm wide beads spaced at 150mm (3/4’ beads @ 12”). Follow manufacturers’ written instructions

.2	Install insulation in moderate contact, stagger end joints to provide a smooth surface for application of membrane.

.3	Install only as much insulation as can be covered by roofing membrane in the same day.

3.4		Self-adhered Base sheet and base Sheet Flashing

.1	Apply adhesive primer by roller at a rate of 5m²/L and allow to cure dry for 30 minutes prior to applying base sheet.

.2	Apply base sheet to prepared substrate. Set in place and pull back release film 150 mm (6") to 300 mm (12") and place on to prepared surface. Remove release film from remainder of sheet and apply contact to sheet as the sheet is being unrolled to ensure proper contact with the prepared substrate. Overlap 75 mm (3") on side laps and 150 mm (6") on end laps. Treat end laps by heating with flame to melt polyfilm.	Offset end laps by 450mm (18”) minimum.

.3	On flashing, offset laps from those of field base sheet by 1/3.  Begin application 100 mm (4") from base of wall and extend vertically as indicated. Mechanically fasten base sheet flashing termination using 25 mm (1") round top nails on 200 mm (8") centres. Refer to manufacturers standard details.

3.6		Torch applied cap sheets

.1 	Prior to installation of torch applied membrane, remove all flammable adhesives and primers from the area.  Clean up all release film.

.2	Roll out and align cap sheet membrane beginning at the low point of the roof or center of the drain. Offset side laps of the cap sheet from those of the base sheet by a minimum of 300mm (12”). Re-roll half way and torch apply to base sheet following manufacturers printed instructions.

.2	Carry to vertical as indicated on drawings.

3.7		Torch applied cap sheet flashings: Offset joints from those of field cap sheet by half and a minimum of 300mm (12”).  Begin application 150 mm (6") from toe of cant or vertical and extend vertically as indicated on drawings.

3.8		Clean Up

Promptly clean up and remove from roof all packaging, cuttings, debris etc in preparation for installation of metal flashings.

END OF SECTION

# Text boxes

Spec Note:	For standard applications specify 2.5.1.

For projects where a low odour, 0 g/L VOC free adhesive is required, such as on LEED projects or where sensitivity to solvent odour may exist, specify 2.5.2

Spec Note:  Where frequent roof traffic is expected or where greater puncture and abuse resistance is required, include section 2.6.2 Roof Coverboard.

Spec Note: For a heavy Duty System where greatest strength and puncture resistance are desired chose 2.8.1;  For an economical alternative chose 2.8.2

Spec Note:	Apply adhesive primer to all Wood and Concrete surfaces.

Clean, oil free Steel decks generally do not require adhesive primer above 5°C.  For applications below 5°C use Adhesive Primer